HPL and Gap Specification

HPL

Roughness	Ra = 0.1Micro meters

Resistivity corrected for temperature 20degC and Humidity

Consult PV`s comment below

https://rpc-cms-re4-upscope.web.cern.ch/rpc-cms-re4-upscope/RPC/Chamber%20production/Components/HPL/QualityAssurance/Resistivity/RPC_Upscope_30Nov2010.pdf

Specifically pages 8 & 9

Average/ sheet		=  	1 – 6 x 10 ˆ10 Ohm.cm

StDev/Av Rho		≤	0.5

Photo Qualification of cleaning by GT, before and after. One side is cleaned for the improved quality bonding of the spacers, but we should be sure that the graphite face is properly degreased either in GT and/or in Kodel to help avoid the “BaBar effect”

Thickness 				=  	2mm ± 50 Micro meters (?)

Dimensions of the cutouts after cutting including the position wrt the raw panel to avoid the edge effects.

Flatness and waviness		=	5mm/m	( to be determined )

Dielectric constant			= 	20 -30  (Paolo Vitulo)

Temperature coefficient of resistivity 		?

Gap Specification

Oiling polymerization			Chloroform test

Oil thickness				≤	2-5 micrometers

Oil appearance (visual inspection )especially runs around spacers

Current/ Voltage characteristics at the Gap production facility

stable current			≤	20% / 30 days	(check with Lee)

Max current			≤	3microAmps @ 9.5kV using gas composition of 			=	0.3% SF6

=	4% C4H10

=	95.7% C2H2F4 (R134a)

OR if using a gas composition of		=	96%R134a

=	4% C4H10

Max current				=	XXmicroAmps @ 9.XXXkV

Graphite Resistivity		150kOhm/sq  	≤  RhoSurface  ≤	200kOhm/sq

Graphite distance from edge of HPL		=25mm

Graphite scratch resistance			=?

Insulation thickness				= 200microns

Outer Edge Material				=PC (GT) or Tape ?(KODEL)

HV connexion and cable		4mm protuberance, PC and 20Kv cable

Dia (Red)

“0V” cable and connexion 		0.2mm above surface and O.25mm2 section

Total thickness of Gap 		=  7mm   ±  0.2mm (?)

Spacer bond test performed on each batch of HPL	≥  30kgf

Spacer test done under gas 		=		(20mbar)

Spacer dimensions

Spacer roughness and material

Final dimensions (as built) of Gap to be sure they fit in the mechanics

Gas inlet/outlet connexions are fully open

Gas connexion orientation 	(see Diag)

Ian crotty

9 Dec 2010