## Slide 1: GT expedition to check on PU contamination as reported by KODEL
Paolo Vitulo
Ian Crotty
23/4 February 2012

## Slide 2: Contents
Sample inspection before cleaning(from Riva)
Cleaning with Acetone, IPA, MEK.
Compression of Kraft onto HPL.
Abrasion of layers.

## Slide 3: Sampling from Batch
22 sheets were inspected from the box of 360.? Probability of find a missing a bad one with 90% bad while taking 10 samples,
= x 10^-9
All were found to be “clean from cutting”.
That is there is some dust in the areas of the cut.
Bakelite is very shiny making it difficult to focus on the surface with a camera.
Bar Code example; 8E19E111215020793

## Slide 4: Layout of (9)test areas
3 methods of cleaning;
Pour on & leave to evaporate
Pour on wipe immediately
Wipe with wet cleaning paper.
Temperature in the shade ~16degC
Acetone
MEK
IPA
Bar Code: 8E19E111215020793

## Slide 5: Cleaning with Acetone
Acetone (from a squeeze bottle) after evaporation leaves fine deposits as shown. These can be readily removed with IPA.
Wiping off the Acetone left a clean surface with no marks

## Slide 6: Cleaning with MEK from clean source
Large pool, 15-20cm) of clean MEK, left to evaporate.

## Slide 7: Cleaning with MEK from clean source
Interference patterns after evaporation

## Slide 8: Cleaning with IPA

## Slide 9: Conclusion after cleaning with Acetone,MEK & IPA
In all 3 cases the wiping method removes all traces.
In the evaporating pool method ;
Acetone leaves small round dry deposits.
MEK leaves dry interference patterns.
IPA leaves the slightest dry deposits.
The slightest wipe with paper & IPA removes all marks.

## Slide 10: Will the kraft paper stick to the HPL due to panels remaining wet while packing them ?
Kraft paper soaked in one of the 3 solvents and enclosed uner PE sheet .
Weights were applied over night

## Slide 11: No sticking of papers to HPL
The paper is released leaving almost no traces

## Slide 12: Is there anything leaching out of the HPL and remaining on the surface ?
Abrading with MEK from the GT cleaning machine & “Scotch Bright”
Cleaning with IPA
Clean dry & dull finish
Also vigorously with the 2 other solvents

## Slide 13: Going into the melamine layer of the HPL
Using 125 abrasive paper some small quantity of the melamine surface was taken for analysis. We will have these with the week
The surface is dry, no leaching of “oil” type products

## Slide 14: Going to the Phenolic core
Melamine extent
Phenolic layer
Again another sample (phenolic) was taken for analysis
Still no leaching of a “wetting” or “dirty” substance coming from within the HPL core. This procedure was performed on both faces of the HPL.

## Slide 15: Conclusions
The sheets(of one box) of HPL delivered from Riva, after cutting, are clean except for the usual dust due to milling out the various formats.
Cleaning with Acetone, MEK or IPA produces a good clean (to the eye) surface.
Kraft paper does not tend to stick to the HPL due to it being wet & compressed with any of the 3 solvents, including the MEK from the GT machine.
4 different levels (superficial, dulling of the mirror finish, abrading of melamine and finally grinding into the core of the panel) of the HPL were tested for leaching of any dirty or oily type products. None were observed by eye.
Samples of the MEK in the GT machine, the roller material, the bristles of the brush, the powder from the upper(melamine) abrading and the core of the HPL have been sent for analysis at CERN labs. None of the samples taken in GT have yet been analysed since their delivery this Monday.

## Slide 16: GT damaged due to snow !!

## Slide 17: Other photos
http://rpc-cms-re4-upscope.web.cern.ch/rpc-cms-re4-upscope/RPC/Chamber%20production/Components/HPL/CleaningGT/GTVisit2324Feb2012/

## Slide 18: Wild goose chasse
http://www.phrases.org.uk/meanings/wild-goose-chase.html